## Slide 1: State Estimation of Cylindrical Cells Using Strain and Pressure Sensors
Gregor Glanz AIT Austrian Institute of Technology
11.02.2026

## Slide 2: Motivation
The state of a Lithium-Ion battery (LIB) in a battery pack is currently determined with the electrical two-pole behaviour.
Battery management system (BMS) measures voltages, currents & temperatures.
Mechanical state of the battery is difficult to determine based on electrical properties.
Figure 1: Swollen laptop battery
Additional Sensors are needed to determine mechanical properties and detect safety critical states.

## Slide 3: Theoretical Background – LIB
LIBs undergo mechanical property changes during their life cycle.
Reversible and irreversible mechanical changes occur during charging and discharging.
Especially the anode (graphite) expands up to ~ 10% during charging (> for Si doped anodes)
Figure 2: Intercalation Stages of Graphite [1]
It is expected, that cell expands during charge  increase in measured strain and contracts during discharge  decrease in measured strain
Can we correlate strain measurements with SOC for different cell types?
Figure 4: Applied Strain Gage on Cylindrical Cell
Figure 3: Schematic drawing of cylindrical cell [2]
[1] G. Bree et al., “Monitoring state of charge and volume expansion in lithium-ion batteries: an approach using surface mounted thin-film graphene sensors,” RSC Adv., vol. 13, no. 10, pp. 7045–7054, Feb. 2023, doi: 10.1039/D2RA07572E. [2] H. Popp et al., “Mechanical methods for state determination of Lithium-Ion secondary batteries: A review,” J. Energy Storage, vol. 31, p. 101859, Sep. 2020, doi: 10.1016/j.est.2020.101859.

## Slide 4: Experimental Setup
Linear Strain gage applied at SOC 0
Circumferential (hoop) strain measured
Measurements conducted in a climatic chamber to minimize environmental temperature influence
Temperature sensor placed on surface to track cells temperature
Amplifier from HBM used: Wheatstone Bridge in Quarter Bridge Configuration
Figure 5: Experimental setup [3]
[3] Glanz et al., J. Electrochem. Soc., 2026; manuscript in preparation

## Slide 5: Samsung 35E
Strain gage placed at the axial centre position
Measurements conducted at room temperature (25°C)
3 different C-rates (0.1C, 0.5C & 1C)
Figure 6: Measurement results of Samsung 35E
  Results
  Increase in strain during charging, decrease during discharging
  Aligns with observations in literature
  Maximum Strain of 450 µε (0.1C)
  Due to temperature increase higher strain measured at higher C-rate

## Slide 6: Samsung 35E
Figure 7: Measurement results for Samsung 35E of 0.1C at two different positions
Various positions investigated  strain gage at bottom position (negative pole)
Almost constant shift in amplitude over whole SOC range  only small deviations close to SOC 0
Various 35E cells at different positions measured  all cells show similar strain behaviour

## Slide 7: Samsung 29E
Figure 8: Measurement results of Samsung 29E
Strain gage placed at the axial centre position
Measurements conducted at room temperature
Two different C-rates (0.1C & 0.5C)
  Results
  Inverse strain behaviour measured: decrease during discharging increase during charging
  Does not align with underlying electro-chemical theory
  Negative Strain at SOC100 of around – 50µε measured
?

## Slide 8: Samsung 29E
Different strain positions investigated
Only at bottom position expected strain behaviour measured  increase during charging and decrease during discharging
Figure 9: Measurement results of Samsung 29E

## Slide 9: Samsung 29E
Different strain positions investigated
Only at bottom position expected strain behaviour measured  increase during charging and decrease during discharging
Figure 9: Measurement results of Samsung 29E

## Slide 10: Samsung 29E
Figure 9: Measurement results of three different Samsung 29E
Different strain positions investigated
Only at bottom position expected strain behaviour measured  increase during charging and decrease during discharging
Measurements conducted on 3 different cells at the bottom position
Cycled at 0.1C to minimize temperature influences
2 out of 3 cells show inverse strain behaviour also at bottom position
What causes this strain behaviour / non uniform expansion?

## Slide 11: Postmortem Analysis to investigate different Strain Behaviours
Assumption: internal structure of Samsung cells is different  especially the tabs
Opened cells in Glovebox under argon-atmosphere
Exactly same tabs were used (height, width, thickness)
Figure 10: Postmortem analysis of Samsung 35 and Samsung 29E
Samsung 29E
Samsung 35E
XRF measurements on anode material conducted: 35E cell  silicon present 29E cell  no silicon present
 More uniform expansion in Samsung 35E due to silicon
a)
b)
a)
b)
d)
c)
d)
c)

## Slide 12: Analysis of internal structure – Samsung 35E & Samsung 29E
CT-Scans conducted in discharged state (SOC0)
Figure 11: CT scans at center position of Samsung 35E and 29E [3]
Samsung 29E
Samsung 35E
[3] Glanz et al., J. Electrochem. Soc., 2026; manuscript in preparation
Samsung 35E small gap between end of active material and housing
Samsung 29E multiple gaps: housing and jelly roll cathode tab in general, bigger gaps
Combination of silicon in anode material and no gaps causes non-position dependent strain results for 35E cell

## Slide 13: Abusive Testing – Overcharge Samsung 35E
Overcharged with 0.5C
CID activated
Measured strain exceeds drastically maximum strain value at SOC100
Strain increases exponentially prior to measured temperature on the cells surface  Detection of safety critical condition with strain gage prior to temperature sensor possible
Figure 13: Overcharge test of Samsung 35E [3]
4.2V
[3] Glanz et al., J. Electrochem. Soc., 2026; manuscript in preparation

## Slide 14: Abusive Testing – Overcharge Samsung 29E
Overcharged with 0.5C
Strain gages applied on 3 different positions (bottom, middle, top)
CID activated
Measured strain is different for each position
Detection of safety critical condition with strain gage prior to temperature sensor not possible
Figure 13: Overcharge test of Samsung 29E [3]
[3] Glanz et al., J. Electrochem. Soc., 2026; manuscript in preparation
4.2V

## Slide 15: Conclusions
Correlation between strain and SOC is not possible for all cell types
For certain cell types SOC estimation possible (ML-estimator developed)
Used active material (Si – content), packaging and manufacturing process are crucial parameters for measuring reproducible strain results
Safety critical states (overcharging) can be detected prior to standard temperature sensors without extensive characterisation (for certain cells)

## Slide 16
Gregor Glanz
Gregor.Glanz@ait.ac.at

## Slide 17: Additional Slides
Figure: Three different parts of the strain gage application device and device

## Slide 18: Additional Slides
Figure: Cell holder for cycling